Proposal of enterprise standart

	
	
	

	Svitap J.H.J.
	Material data sheet
	PND 72-012.10-11

	Komenského 75
	Artificial leatherette
	

	768 11 Chropyně
	Vinytol 635
	SKP 17543710/

	Czech republic
	
	

	This technical data sheet is joined to the standard ČSN 64 7003 Synthetic Leathers.Artificial Leathers and sets the underlaying material, characteristics and appropriate particular demads for Vinytol 635.  

	Underlaying material
	Type
	Elastic knitting 

	material
	Structure
	100 % PES

	Characteristic


	Unit
	Value
	Tested accord. to

	Surface area mass
	kg.m-2
	0,620 ( 0,030
	ČSN 64 7011

	Width
	cm
	97 ± 2
	ČSN 64 7010

	Thickness 
	mm
	1,30 ± 0,10
	area (
press 

	Power at break
	lengtways
	N/5cm
	160
	ČSN 64 7012

	
	across
	
	80
	    

	Elogation at break
	lengtways
	%
	60
	

	
	across
	
	110
	   

	Resistance to further cracking      x/
	lengtways
	N
	25
	ČSN 64 7032

	
	across
	
	25
	

	Cohesion of layers
	N.m-1
	500
	ČSN 64 7030

	Resistance against reapeted bend  + 23 C
	kc/st/st
	5/5/5
	ČSN 64 7029

	Suitability in the temperature range       x/
	oC
	- 18 till +60
	

	Non-tolerant values set in the Technicial data sheet are the guaranteed lowest value.

x/    specification for informative values

xx/  specification for type tests, made at the introducing into production, material change or   

       technology.

Recommended application: back side of sport matress 

	Approved for producer:

....................          ...................................

    date                      signature + stamp
	Approved for customer:

....................          ...................................

     date                    signature + stamp



	It substitutes
	Force up to date:

5th May 2008
	Exploiter:department

Development and quality
	Copy No. 4

	
	
	
	Page: 1


