Enterprise standart                                      

	
	
	

	SVITAP J.H.J.
	Material data sheet
	PND 01-001.25-13

	Komenského 75
	Meshing coating PVC textilie
	

	768 11 Chropyně
	Vinytol 312 N HYGH
	SKP 17.54.37.

	Czech republic
	
	

	This technical data sheetis joined to the standard ČSN 64 7003 Synthetic Leathers.Artificial Leathers and sets the underlaying material, characteristics and appropriate particular demads for Pervinyl 312 N HYGH.  

	Underlaying material
	Type
	Polyester silk 1100 dtex 60 Z

	
	Texture on 1 cm
	Warp  2,0 x 2 ( 5%

Weft   2,0       ( 5%

	Characteristic


	Unit
	Value
	Tested accord. to

	Surface area mass
	kg.m-2
	0,310 ( 0,030
	EN ISO 2286

	Width
	cm
	100 - 120 + 2
	EN ISO 1773

	Power at break
	lengtways
	N/5cm
	1500
	EN ISO 13934-1

	
	across
	
	1000
	

	Elogation at break
	lengtways
	%
	35
	

	
	across
	
	35
	   

	Determination of Phthalic acid esters
	%
	<0,001
	EN 14372

	Flamability at most                               xx/    
	mm.min-1
	M3
	FD P 92-507

	Flamability at most                               xx/    
	mm.min-1
	100
	EN ISO 3795

	Suitability in the temperature range       x/
	oC
	- 20 till +50
	

	Non-tolerant values set in the Technicial data sheet are the guaranteed lowest value.

x/    specification for informative values

xx/  specification for type tests, made at the introducing into production, material change or   

       technology.

Notice: For production are not used raw material according to regulation ChildCare Regulation   

             (DE_2005/84/CE) and shedule of REACH.
Recommended application: material for production deckchair for children till 3 years.

	Approved for producer:

....................          ...................................

    date                      signature + stamp
	Approved for customer:

....................          ...................................

     date                    signature + stamp



	It substitutes
	Force up to date:

5th February 2014
	Exploiter:department

Development and quality
	Copy No. 4

	
	
	
	Page: 1


